## Slide 1
http://en.wikipedia.org/wiki/Atomic_force_microscopy
M. Cain, Springer, Characterization of ferroelectric bulk materials and thin films
AFM HEAD
SLIDING RACK
(X,Y)
Asylum MFP-3D AFM
Asylum Research MFP-3D Users Manual
TIP
CANTILEVER
Sample
Tip
Laser beam
Cantilever
Atomic force microscopy (AFM)
MODES:
AFM (contact, tapping)
Piezo-response force microscopy (PFM)
Conductive AFM (CAFM)
Kelvin-probe force microscopy (KPFM)
Electrostatic-force microscopy (EFM)
Magnetic force microscopy (MFM)
Scanning thermal microscopy (SThM)-NEW

## Slide 2
Piezo-response force microscopy (PFM)
the voltage applied to the scanning tip in contact mode
conductive tip: (usually Si tip on Si cantilever, coated with Ti/Ir or Pt)
tip diameter: 7 nm to 30 nm
Driving signal: V = Vac cos(ωt)
Piezoresponse Force Microscopy with Asylum Research AFMs, S. Jesse, ORNL
PROKSCH, R. in KALININ, S. Piezoresponse Force Microscopy with Asylum Research AFMs, Users Manual.
VERTICAL AND LATERAL DIRECTIONS
http://www.ntmdt.com
Kalinin et al., Microsc. Microanal. 12, 2006.

## Slide 3
Topography
domain boundaries
no response (black line)
Periodically poled lithium niobate
5 mm
A) Vertical PFM mode-example
PFM vertical amplitude image
PFM vertical phase image

## Slide 4
5 mm
5
0
25
20
15
10
nm
height
Pb(Sc0.5Nb0.5)O3 ceramics
Topography
vertical
A) Vertical PFM mode-example
PFM vertical amplitude image
PFM vertical phase image

## Slide 5
Periodically poled lithium niobate
PFM lateral amplitude
image
PFM lateral phase
image
no signal in lateral direction
Topography
5 mm
PFM vertical amplitude image
PFM vertical phase image
C) Vector PFM mode (vertical and lateral directions)

## Slide 6
BiFeO3 ceramics
by rotating the ceramic sample
for 90°
VERTICAL Z
LATERAL Y
LATERAL X
C) Vector PFM mode (vertical and lateral directions)
T. Rojac, H. Uršič et al., Adv. Fun. Mat. 2015